. LAYER FOR DRAINAGE AND WATER STORAGE

Supply and installation of:

DAKU FSD 20 components, which are rigid sheets made of sintered expanded polystyrene foam. They are produced with materials free from regenerated elements. They are of white color, barely flammable and their raw mass is of 25 kg/m3. All DAKU FSD 20 components comply with UNI 11235:2015 standards. They perform a threefold function of mechanical protection of the waterproof surface (does not require a separating layer), water drainage and water storage.

Technical data:

| - Dimensions | 1000 x 1250 mm |  |
| --- | --- | --- |
| - Thickness | 82 mm |  |
| - Density | 25 Kg/mc (+/-10%) |  |
| - Maximum water storage capacity | 13,1 liters/sqm ca. |  |
| - Gap between water and filter | 10 mm |  |
| - Free air volume at maximum water storage capacity | 21,5 liters/sqm |  |
| - Drainage capacity at 20 kPa with i=0.01 with rigid / rigid bedding (R/R option) |  |  |
| longitudinal | 1,46 l/ms | (EN ISO 12958) |
| transversal | 1,44 l/ms | (EN ISO 12958) |
| - Drainage capacity at 20 kPa with i=0.1 with rigid / rigid bedding (R/R option) |  |  |
| longitudinal | 4,95 l/ms | (EN ISO 12958) |
| transversal | 4,90 l/ms | (EN ISO 12958) |
| - Vertical drainage capacity | 0,73 l/sqms | (EN ISO 11058) |
| - Thermal dispersion resistance K | 0,71 sqm x K/W |  |
| - Thermal conductivity | 0,034 W/mK | (UNI EN 12667) |
| - Height of support feet | 20 mm |  |
| - Number of support feet | 252 pz |  |
| - Support surface | 2.052 csqm/sqm |  |
| - Flammability Class | E | (EN 13051) |

The installation of the DAKU FSD 20 components is made directly on the insulation/waterproof surface.

sqm ca. 0.00