. FILLING LAYER

Supply and installation of:

DAKU FLT 120 which is a white non-woven fabric geotextile made of highly tenacious polypropylene. The fabric is treated with UV rays, needled, calendered, glue-free, rot-proof, resistant to micro-organisms and without recycled materials. It is used as a filling layer and as a mechanical protection component.

Technical data:

| - Roll Dimensions | 2,00 x 50 m (100 sqm) |  |
| --- | --- | --- |
| - Mass | 120 gr/mq (+/-10%) | (EN ISO 9864) |
| - Thickness at 2kPa | 0,80 mm (+/-20%) | (EN ISO 9863-1) |
| - Tensile strength: |  |  |
| longitudinal | 9,0 Kn/m (-10%) | (EN ISO 10319) |
| transversal | 9,0 Kn/m (-10%) | (EN ISO 10319) |
| - Elongation at maximum load: |  |  |
| longitudinal | 55% (+/-30%) | (EN ISO 10319) |
| transversal | 60% (+/-30%) | (EN ISO 10319) |
| - Static puncture resistance | 1,50 kN (-10%) | (EN ISO 12236) |
| - Dynamic puncture resistance | 32 mm (+20%) | (EN ISO 13433) |
| - Velocity index VIH=50: | 115 mm/s (-30%) | (EN ISO 11058) |
| - Horizontal flow capacity: | 0,80x10-3 l/ms (-30%) | (EN ISO 12958) |
| - Characteristic opening size d=90%: | 0,11 mm (+/-30%) | (EN ISO 12956) |
| - Resistance to oxidation: | min. 25 years | (EN ISO 12956) |

DAKU FLT geotextiles are installed directly on the insulation/waterproof surface, overlapping the sheets for 10 cm and folding them on the vertical edges of the surfaces for a height equal to the one of the DAKU FSD/DAKU DRAIN components or of the paved surface/protection blocks.

sqm² 0.00