. PRE-FILTER LAYER - FILLING

Supply and installation of:

DAKU LAPILLO 5/10, consisting of an inert layer based on alveolar lava lapillus with open cells, non-toxic, free from crystalline free silica and active limestone. It can allow the creation of separation, mulching, filter, water accumulation or filling layers in the DAKU stratigraphies for green roofs. DAKU LAPILLO 5/10 complies with the requirements of the UNI 11235: 2015 standard for the construction of accumulation layers in granular aggregates.

Technical data:

| - Granulometry | 5-10 mm (mixed variable) |  |
| --- | --- | --- |
| - Apparent density (pit humidity) | 880-980 Kg/m3 |  |
| - Water retention | 8-13% v/v |  |
| - Water available | 6-9% v/v |  |
| - PH | 7-8 |  |

* DAKU LAPILLO is made of natural materials; the values listed above are gross and do not represent a contract obligation.

The installation is made by hand above the DAKU STABILFILTER components for filtering and filling, with a thickness of…… cm compacted.

The material will be supplied unpackaged

The material will be supplied in 33l bags

The materials will be supplied in “Big Bags” (1 m3)

m3 0,00