. FILTERING AND STABILIZATION COMPONENT

Supply and installation of:

DAKU STABILFILTER SFI, which is a non-woven geotextile in polypropylene fibers. It is 1.50 mm thick (EN 9863-1), needled and ironed without glues or chemical elements. DAKU STABILFILTER SFI comply with the UNI 11235:2015 standards. It is used as a separation layer and as a filter between the drainage/storage components (DAKU DRAIN/FSD) and the DAKU LAPILLO filling layer or the DAKU ROOF SOIL components on the intensive gardens. DAKU STABILFILTER SFI divides and distributes water, allowing the DAKU ROOF SOIL substrate to gradually absorb it.

Technical data:

| - Roll Dimension (rotolo) | 2,00 x 50 m (100 sqm) |  |
| --- | --- | --- |
| - Areal density | 260 gr/mq. (+/-10%) | (EN ISO 9864) |
| - Thickness at 2kPa | 1,50 mm (+/-20%) | (EN ISO 9863-1) |
| - Tensile strength: |  |  |
| longitudinal | 21 Kn/m (-10%) | (EN ISO 10319) |
| transversal | 21 Kn/m (-10%) | (EN ISO 10319) |
| - Elongation at maximum load: |  |  |
| longitudinal | 65% (+/-30%) | (EN ISO 10319) |
| transversal | 70% (+/-30%) | (EN ISO 10319) |
| - Deformation at working load, Long. - Trasv: | < 20% |  |
| - Static puncture resistance CBR | 3200 N (-10%) | (EN ISO 12236) |
| - Dynamic puncture resistance “cone drop” | 14 mm (+20%) | (EN ISO 13433) |
| - Velocity index VIH=50 | 75 mm/s (-30%) | (EN ISO 11058) |
| - Horizontal flow capacity | 2,30 x 10-3 l/ms (-30%) | (EN ISO 12958) |
| - Characteristic opening size d=90% | 0,07 mm (+/-30%) | (EN ISO 12956) |
| - Resistance to oxidation | min. 25 years | (EN ISO 12956) |

DAKU STABILFILTER SFI is installed on the DAKU DRAIN or FSD components, surmounting the sheets of about 10 cm and folding them on the vertical edges of the surface for a height equal to the thickness of the DAKU LAPILLO filling layer or of the DAKU ROOF SOIL substrate.

sqm ca. 0.00