. SUPPORTING COMPONENT

Supply and installation of:

DAKU GRID 4, which is a bi-oriented polypropylene geogrid, black in color, with a quadrangular shape. The geogrid is built using co-extrusion and biaxial ironing techniques. The geogrid is used on pitched roofs, with a sloping between 15° and 25° (+/-15%). It performs as a basic reinforcement to install the DAKU GEO (75 and 100) containment components for the DAKU ROOF SOIL substrate.

Technical data:

| - aperture size MD | 40 mm | (typical values) |
| --- | --- | --- |
| - aperture size TD | 27 mm | (typical values) |
| - Strenght at 2% strain | 10,50 KN/m | ISO 10319 |
| - Strenght at 5% strain | 21,00 KN/m | ISO 10319 |
| - Peak Tensile strength | 30.00 KN/m | ISO 10319 |
| - Yield point elongation | 11.0% (MD), 10.0% (TD) | ISO 10319 |

DAKU GRID 4 is installed above the DAKU STABILFILTER substrate, before the installation of the DAKU GEO substrate. DAKU GRID 4 and DAKU GEO are tied together with nylon stripes, before the substrate is installed. DAKU GRID 4 must be anchored on top of the water storage component or on its the intermediate points.

sqm 0,00