. SUPPORTING COMPONENT

Supply and installation of:

DAKU GRID 5, which is a bi-oriented polypropylene geogrid, black in color, with a quadrangular shape. The geogrid is built using co-extrusion and biaxial ironing techniques. The geogrid has a bi-oriented tridimensional structure with thick wires that have a concave section, meaning that it can uniformly sustain weights. It is used as a functional support for the DAKU SAFETY POINT anti-fall system.

Technical data:

| - Rib Thickness | 2.00 mm (TD), 3.50 mm (MD) | (typical values) |
| --- | --- | --- |
| - Junction thickness | 7,00 mm | (typical values) |
| - Aperture size | 55 mm | (typical values) |
| - Resistance to weathering | 100% | EN 12224 |
| - Stiffness at 0,5% strain | 900 – 600 KN/m | ISO 10319 |

DAKU GRID 5 is installed after the DAKU DRAIN/DAKU FSD components and before the DAKU STABILFILTER substrate. It will be properly locked between the concrete base-plate and the steel plate of the DAKU SAFETY POINT system.

sqm 0,00