. LAYER FOR DRAINAGE AND WATER STORAGE

Supply and installation of:

DAKU DRAIN 35 components, which are rigid sheets made of sintered expanded polystyrene foam. They are produced with materials free from regenerated elements. They are of white color, barely flammable and their raw mass is of 35 kg/m3. All DAKU DRAIN 35 components comply with UNI 11235:2015 standards. They are used for the mechanical protection of the waterproof surface (does not require a separating layer) and for the water drainage

Technical data:

| - Dimensions | 1000 x 1250 mm |  |
| --- | --- | --- |
| - Thickness | 47 mm |  |
| - Density | 35 Kg/mc (+/-10%) |  |
| - Drainage capacity at 20 kPa with i=0.01 |  |  |
| longitudinal | 1,46 l/ms | (EN ISO 12958) |
| transversal | 1,44 l/ms | (EN ISO 12958) |
| - Drainage capacity at 20 kPa with i=0.1 |  |  |
| longitudinal | 4,95 l/ms | (EN ISO 12958) |
| transversal | 4,90 l/ms | (EN ISO 12958) |
| - Vertical drainage capacity | 14,74 l/mqs | (EN ISO 11058) |
| - Thermal dispersion resistance K | 0,71 mq x K/W |  |
| - Thermal conductivity | 0,034 W/mK | (UNI EN 12667) |
| - Height of support feet | 20 mm |  |
| - Number of support feet | 252 pz |  |
| - Support surface | 2.052 cmq/mq |  |
| - Flammability Class | E | (EN 13051) |

The installation of the DAKU DRAIN 35 components is made directly on the insulation/waterproof surface.

sqm ca. 0.00